Product Group:	LANscape® FutureCom

Product:		F/FTP 450/23, 4-pairs, LSZH-3

### Product Description

The FutureCom F/FTP 450/23 cable is specified for applications up to 450 MHz and exceeds the defined Category 6 according to EN 50288-5-1. Outstanding system headrooms of the complete cabling system in compliance with ISO/IEC 11801 (2002) and EN 50173-1 (2003). Outstanding performance for the transmission of digital data signals for future coming applications up to 1GbE in compliance with Class E. The low skew (delay difference) between the pairs underlines their suitability for future 1 Gigabit Ethernet applications.

### Cable Requirements (Characteristics)

Diameter of copper conductor AWG 23, wire insulation is halogen free. Each twisted pair is individually shielded with a metal foil (PiMF). Tinned ground wire centrically running in. Complete shielding with metal foil. Sheath material is halogen-free; flame retardant to IEC60332-1 and EN 50266-2-1; low smoke to IEC61034; non corrosive to IEC60754-2 and EN 50267; outer sheath colour is blue.

Tensile strength >145 N, fire rating 0.58 MJ/m, outer diameter 7.2 mm, weight approx. 48 kg/1,000 mtrs.

Bending radius during installation > 60 mm; Bending radius during operation:  > 22 mm.

### Temperature range during installation 0°C to +50°C; during operation -20°C to +60°C.

Typical impedance Z0 @ 100 MHz: 100 ( 5 Ω

Typical transfer impedance: ( 10 mΩ/m @ 10 MHz

Typical propagation delay ( 10 MHz: 4.2 ns/m, typical delay skew: 4 ns/100m

Frequency	Attenuation       NEXT		PSNEXT	ACR-F	 	PS ACR-F	ACR-N

MHz		dB/100m	dB/100m	dB/100m	dB/100m	dB/100m	db/100m

1		1.8		>100		98		93		91		98.2

10		5.3		>100		98		93		91		94.7

62.5		13.6		97		95		86		84		82.4

100		17.3		95		93		83		81		77.7

450		38.0		85		83		54		52		47.0

Exceeds requirements on 100m installed Category 6 cable (in compliance with EN 50288-5-1)

### General Requirements

The product is delivered in a suitable packing. Special details of delivery. type designation and order numbers have to be available. Further information will be given on request.

### Type Designation

### Corning FutureCom  F/FTP 450/23 4P LSZH-3

### Order Information

CCXDDA-D0047-C001-L7

Shipping Length:

1.000 m on one way drum

Quantity (unit)	:		___

Price		:		___

Lump Sum Price	:		___